## Slide 1
PRESENTED BY
Green Tribology
Biodegradable oil Enhancement Techniques
ME 698 T
Term paper presentation
Chinmay Pratap
Devabrata Bothra
Amrit Kalash
Harsh Shah
Kartikeya Pandey
Dr. Manjesh K. Singh
Instructor

## Slide 2
  Introduction
  Experimental Setup and Surface preparation
  Data Processing and Findings
  Results and Findings
  Conclusion
  References
  Acknowledgement
Contents

## Slide 3
  Green Tribology is defined as the science and technology of the tribological aspects of ecological balance and of environmental impacts.
  With the viewpoint of sustainable development of resources and environment, the main objectives of green tribology are:
1. the environment-friendly saving of energy and materials,
2. the enhancement of the environment and quality of life.
  Our project delves into the lubrication aspect of tribology and tries to address the current challenges from the point of view of green tribology.
Introduction

## Slide 4
Purpose of Lubrication:
  Reduce friction between moving surfaces via a low shear strength film.
  Conventional Lubricants:
Mineral oils, synthetic oils, and greases
Non-biodegradable → Harmful effects:
  Water contamination
  Soil degradation
  Toxicity to aquatic life
Sustainable Alternative:
  Plant-based lubricants
  Biodegradable
  Environmentally safe
Introduction (cont’d)

## Slide 5
Biodegradable Lubricant Used:
  Mustard oil.
  Goal: Analyze Coefficient of Friction (COF) between 2 steel samples using Linear Reciprocating Tribometer at 2 different temperatures.
  Addition of MoS₂ nanoparticles as a solid lubricant.
  Observe its effect on COF values.
Introduction (cont’d)

## Slide 6
1. Polishing Stage
  Equipment: Wet polishing machine (200 RPM), 320 & 1200-grit abrasives
  Purpose: Smooth, uniform surface on SS304 plate
  Why: Ensures consistent surface finish, minimizing artifacts in friction/wear tests
2. Cleaning Process
  Method: Acetone cleaning post-polishing
  Why: Removes oil, debris, and abrasive residues for contamination-free testing
Experimental Setup & Surface Preparation
Fig: Schematic diagram

## Slide 7
1. Hand Stirring
  0.05g, 0.25g, 0.5g of MoS₂ added to 50 ml mustard oil → 0.1%, 0.5%, 1.0% solutions.
  Reason: Initial dispersion of MoS₂.
Experimental Setup & Surface Preparation
2. Ultrasonic Bath
  Conditions: 44 °C for 20 minutes
  Purpose: Final homogenization of MoS₂ in mustard oil
  Why: Breaks agglomerates from manual/magnetic stirring to ensure uniform, stable MoS₂ dispersion
3. Magnetic Stirring (30°C, 10 mins)​ at 500 RPM
  Purpose: Homogenize solution.​
  Reason: Prevent clumping of particles.

## Slide 8
Visual Appearance
  Uniform dark gray to black (varies with MoS₂ concentration)
  Smooth consistency; no visible sedimentation or clumps
  Slight metallic shimmer due to nano-MoS₂ dispersion
Stability Indicators
  No floating particles or undissolved flakes
  Homogeneous color, even after swirling
  Noticeable viscosity increase at higher MoS₂ wt%
Experimental Setup & Surface Preparation
Fig: Before adding MoS2
Fig: After adding MoS2

## Slide 9
Tribometer Parameters
  Specimen: SS304 plate + AISI 52100 ball.
  Load: 5 N
  Principal Hertizian Stress: 1199.3 MPa
  Frequency: 4 Hz
  Stroke Length: 2 mm
  Temperature: 30°C (Room Temp), 80°C (Elevated)
  Duration: Fixed time across all tests
  Reasoning: To meet real-world sliding conditions and quantify friction behavior across temp and composition variations at specific parameters.
Linear Reciprocating Tribometer Testing
Experimental Setup & Surface Preparation
Fig: Linear Reciprotating Tribometer

## Slide 10
Experimental Setup & Surface Preparation

## Slide 11
Experimental Setup & Surface Preparation
Rheological Characterization
Observations:
  1% MoS₂ had higher viscosity, but no linear trend in frictional benefit
Tribological Characterization
  Data from Tribometer:
  CoF trends (min @ 0.1%, rise at 0.5%)
Post test Characterization method
Fig: SS304 Samples

## Slide 12
Data Processing
  Exported raw data from the software
  Calculated Coefficient of Friction (COF) for each case.
  Plotted COF against temperature variation for comparison and trend analysis.
  Implemented the Rolling average to filter the COF value.
  Measured the average COF value.
Data Processing & Findings
Fig: Code Snippet

## Slide 13
Results and Discussion
Fig: Room Temperature (Pure oil)
Fig: 80 C (Pure oil)

## Slide 14
Results and Discussion
Fig: Room Temperature (0.1 % MoS2)
Fig: 80 C (0.1% MoS2)

## Slide 15
Results and Discussion
Fig: Room Temperature (0.5 % MoS2)
Fig: 80 C (0.5% MoS2)

## Slide 16
Results and Discussion
Fig: Room Temperature (1 % MoS2)
Fig: 80 C (1% MoS2)

## Slide 17
Results and Discussion
Fig: Summary Table

## Slide 18
(i) Average CoF Ranges from 0.109 to 0.135 which is significantly lower than the dry CoF value (0.45~0.6)
(ii) Effect of MoS₂ Concentration:
  Initial MoS₂ addition reduced CoF at both low & high temperatures
  At higher concentrations CoF were higher for lower temperature but were lower for higher temperature
Key Observations
Conclusion
Fig: Plot COF Vs Temp.

## Slide 19
Anomalous Behavior – 0.5 wt% MoS₂ at Room Temperature
  Unlike other samples, CoF did not stabilize
  Displayed a monotonically decreasing trend throughout the test
Key Observations
Error Sources
Possible Causes – 0.5 wt% MoS₂ Anomaly (RT):
  MoS₂ Structure: Layered hexagonal structure increases interparticle interaction → lower dispersion stability at intermediate concentration
  Stability Issue @ RT: 0.5 wt% may be high enough for settling in mustard oil at room temp
  Tribometer Error: Potential heating system malfunction → uneven temperature affecting CoF
  Surface Roughness: Localized anomaly may have disrupted lubricant film
Conclusion

## Slide 20
  Immediate Use: Use samples right after preparation to avoid settling, for later use, samples should be stirred just before the experiment.
  Improve Dispersion:
    If unstable, use a surfactant (e.g., CTAB) to stabilize MoS₂ via electrostatic repulsion
  Heating System Check:
    Ensure proper calibration and uniform heating
    Let tribometer stabilize at set temperature before testing
  Specimen Handling:
    Use fresh specimens whenever possible or at different locations for the same specimen
  Multiple tests should be conducted for same lubricant at similar conditions to avoid any system error.
Conclusion
Prevention Measures

## Slide 21
Conclusion
Industrial Suitability of Natural Lubricant (Mustard Oil + MoS₂)
  Competitive average CoF: 0.11–0.12, comparable to synthetic lubricants (boundary lubrication)
  MoS₂ addition improves anti-wear, load capacity & friction reduction
  Natural lubricity from fatty acids enhances wettability
  High flash point → lower fire risk in industrial settings
Potential to be used

## Slide 22
  Biodegradable within 28 days (OECD 301B) → minimal long-term pollution
  Non-toxic to aquatic life vs. hazardous mineral oils
  MoS₂: Inert and safe in small concentrations
  Free of PAHs, sulfur compounds, heavy metals → cleaner disposal
  Plant-derived & renewable → reduces reliance on fossil fuels
  Lower life-cycle emissions from production to disposal
Conclusion
Eco-friendly benefits

## Slide 23
Future Direction
Future Direction
Exploring Other Natural Lubricants for Sustainable Tribology
  Aloe Vera Gel & Egg White were also considered as potential natural lubricants
  These bio-based alternatives can be enhanced (e.g., with MoS₂) for improved performance
  Offer eco-friendly, biodegradable, and non-toxic solutions for industrial applications
  Align with goals of sustainable development in real-world tribological systems
  Promote low environmental impact and reduced pollution in lubrication technology
More Eco-friendly Lubricants

## Slide 24
Future Direction
References
1] Y. Hori, “A theory of oil whip”, 1959.
[2] W. O. Winer, “Molybdenum disulfide as a lubricant: A reviewof the fundamental knowledge”, Wear, vol. 10, no. 6, pp. 422–452, 1967.
[3] A. Willing, “Lubricants based on renewable resources–an environmentally compatible alternative to mineral oil products”,Chemosphere, vol. 43, no. 1, pp. 89–98, 2001.
[4] S. Boyde, “Green lubricants. environmental benefits and impacts of lubrication”, Green Chemistry, vol. 4, no. 4, pp. 293307, 2002.
[5] J. H. Hamman, “Composition and applications of aloe vera leafgel”, Molecules, vol. 13, no. 8, pp. 1599–1616, 2008.
[6] C. Betton, “Lubricants and their environmental impact”, Chem-istry and technology of lubricants, pp. 435–457, 2010.
[7] M. Nosonovsky and B. Bhushan, Green tribology: Principles,research areas and challenges, 2010.
[8] Bharat. “Wikipedia”. Accessed: 2025-04-05. (2012), [Online].Available: https://en.wikipedia.org/wiki/Tribology.
[9] Available at : https://pubs.acs.org/doi/10.1021/acs.jpcc.8b05922
[10] Availablr at: https://pubs.rsc.org/en/content/articlehtml/2020/ra/d0ra03414

## Slide 25
  We sincerely thank Dr. Manjesh K. Singh for his invaluable guidance and for providing us the opportunity to work on this project.
  Our heartfelt appreciation to the Tribology Lab Team —Mr. Kuldeep, Mr. Ajay, Mr. Susheel, Mr. Arun, and others for their constant support and assistance with the experimental setup.
  We also extend our gratitude to the Department of Mechanical Engineering, IIT Kanpur for offering the platform and resources to carry out this research.
Acknowledgement